HQT93006硫化极压剂

产品简介及适用范围 HQT93006为红棕色清澈低味液体，适用于金属的切削和成型加工，也可用于工业齿轮油、导轨油等的调配。非活性硫，适用有色金属的加工。粘度较低，易乳化，可用于水溶性切削液的配制。 HQT93006 Sulfurized Fatty Ester: EP additive HQT93006 is red brown clear oily liquid, mild oder, used as EP additive for industrial lube and metalworking fluids, such as metal cutting and forming fluids. Inactive type sulfur, suitable for processing non-ferrous metal. It is low viscosity, easy to be emulsified, make it a good choice for formulating water soluble cutting fluid. 项 目 Properties; 质量指标 Test Results; 试验方法 Test Method. 比重（20℃）, g/cm3 Gravity; ≈ 0.975; SH/T 0604. 硫含量 %， Sulfur Content %; ≈ 12.0; ASTM D4294. 铜片腐蚀级别（100℃, 3h） Cu Corrosion Test (100℃, 3h）; ≤ 1a; ASTM D130. 色度，Color; ≤ 8; ASTM D1500. 运动粘度（40℃），mm2/s Viscosity（40℃），mm2/s; ≈ 100; ASTM D445. PBN; 5%; 785; ASTM D2783. 10%; 1020. PDN; 5%; 3089. 10%; 3922. 磨斑直径，mm Wear Diameter; 5%; 0.50; ASTM D4172. 10%; 0.59.